# Product Description

Polyester Solutions CIP Insulation is a range of 100% polyester acoustic insulation products designed for reducing and controlling reverberated noise in building interiors. CIP is ideally suited for use as an absorber behind acoustic panels and ceiling systems. CIP is available in a range of densities and performance options. CIP is supplied as lofted white or black insulation panels /sheets measuring 2400mm x 1200mm (other sizes available on application).

# Applications

# Polyester Solutions CIP Insulation has been engineered to maximize sound absorption for the control of reverberated noise in building interiors. Polyester Solutions CIP Insulation is ideal for managing noise in theatres, studios, auditoriums, halls, offices, retail and indoor swimming pool complexes. Polyester Solutions CIP Insulation can also be used in marine applications, as acoustic baffles, acoustic infill for silencers and louvers, and insulation for Original Equipment Manufacturers (OEM)

# Standard Sizes and Packaging

| PRODUCT | NOMINAL THICKNESS (mm) | NRC1 | Est. R-VALUE (m2/kw) | PACK SIZE2 | m2/PACK |
| --- | --- | --- | --- | --- | --- |
| CIP14-25 | 25mm | 0.50 | R0.48 | 1200mm x 2.4m x 10 Sheets | 28.8m2 |
| CIP 20-25 | 25mm | 0.50 | R0.60 | 1200mm x 2.4m x 10 Sheets | 28.8m2 |
| CIP 32-25 | 25mm | 0.70 | R0.68 | 1200mm x 2.4m x 10 Sheets | 28.8m2 |
| CIP 48-25 | 25mm | 0.65 | R0.73 | 1200mm x 2.4m x 10 Sheets | 28.8m2 |
| CIP 14-50 | 50mm | 0.70 | R0.95 | 1200mm x 2.4m x 5 Sheets | 14.4m2 |
| CIP 20-50 | 50mm | 0.75 | R1.2 | 1200mm x 2.4m x 5 Sheets | 14.4m2 |
| CIP 32-50 | 50mm | 0.80 | R1.36 | 1200mm x 2.4m x 5 Sheets | 14.4m2 |
| CIP 48-50 | 50mm | 0..85 | R1.47 | 1200mm x 2.4m x 5 Sheets | 14.4m2 |
| CIP 20-75 | 75mm | 0.85 | R1.68 | 1200mm x 2.4m x 4 Sheets | 11.5m2 |
| CIP 32-75 | 75mm | 0.90 | R2.03 | 1200mm x 2.4m x 4 Sheets | 11.5m2 |
| CIP 48-75 | 75mm | 1.05 | R2.20 | 1200mm x 2.4m x 3 Sheets | 8.6m2 |
| CIP 20-100 | 100mm | 0.95 | R2.24 | 1200mm x 2.4m x 3 Sheets | 8.6m2 |
| CIP 32-100 | 100mm | 1.00 | R2.64 | 1200mm x 2.4m x 2 Sheets | 5.7m2 |
| CIP 48-100 | 100mm | 1.10 | R2.81 | 1200mm x 2.4m x 2 Sheets | 5.7m2 |

# 2 NRC Noise reduction Coefficient

# 1 Other sizes available on application

# Fire Resistance

When tested in accordance with AS1530.3 (1999), “Early Fire Hazard Properties of Materials”, PSB exhibit the following characteristics:

Ignitability Index			0

Spread of Flame Index			0

Heat Evolved			0

Smoke Developed Index			0 - 3

# Moisture Resistance

Exposure to an atmosphere of 50˚C and 95% relative humidity for 4 days results in less than 0.2% by vol moisture absorption.

# Maximum Service Temperature

The maximum temperature to which Polyester Solutions CIP insulation should be exposed in service is 150˚C.

# Environmental and Health Benefits

Recycled Fibre Content		80% minimum

Volatile Organic Compounds (VOC’s)		No harmful VOC’s

Formaldehyde Content		Nil

Phenol   Content		Nil

Ammonia   Content		Nil

Ozone Depleting Potential (ODP)	Nil

Chloride    Content	Nil

Total Recyclable Content		100%

How to Specify

The insulation material shall be Polyester Solutions CIP  by density and thickness .

General Installation Advice

Polyester Solutions CIP Insulation  is safe and easy to install in walls or ceilings Polyester Solutions CIP  products are easily torn across the width of the products or if required can be cut with a pair of industrial scissors, shears or serrated knife (type Swibo with half moon head. Use safety mesh gloves.) For higher density products use a rotary cutter made to cute textiles (brand type Elizabeth Lightning cutters). Off cuts can be used to fill corners, crevices and gaps, eliminating any waste. For walls, the insulation is placed between the wall studs or furring channels before the plasterboard is put in place. If required, string/strap insulation to secure it into position. No special clothing, gloves or masks required for installation. Allow up to one month for products subjected to compression packing to recover to their nominal thickness.

Testing

All testing was conducted in a laboratory situation. On site results may vary due to site conditions and quality of installation. Thermal testing is done in accordance with AS/NZS 4859.1(Materials for the thermal insulation of buildings - General criteria and technical provisions) and acoustic testing in accordance with ISO 354:2003  Acoustics -- Measurement of sound absorption in a reverberation room. As these products are constantly being researched and developed, we reserve the right to update these specifications without notice.