POLYESTER SOLUTIONS,

WALLBLOCK ACOUSTIC

Premium Choice for Acoustic Insulation

PRODUCT DESCRIPTION

Consumers both commercial and domestic have very good and sound reasons to specify polyester insulation, as much of the raw materials used in the manufacture is recycled material P.E.T (polyethylene terephthalate),(clear plastic beverage containers). No gloves, masks or boiler suits required to handle our range of products.

QUALITY ASSURED

Polyester Solutions Batts are made to the highest standards and comply with the building code of Australia AS/NZS4859.1.

STANDARD SIZE AND PACKAGING

R-Value			Size		Nominal 		Batts			Area (M2)

(m2K/W)			(mm)		 Thickness		per pack		per pack

R1.5		        1170 x 580	      75			    8		          	5.42

R1.5		        1170 x 430	      75			    8			4.02

R2.0	           1170 x 580	      90			    8			5.42

R2.0	           1170 x 430	      90			    8			4.02

R2.5		        1170 x 580	      90		      	    6			4.07

R2.5		        1170 x 430	      90		     	    6			3.02

SOUND ABSORBTION

Product Code	R-Value		Thickness			NRC

(m2K/W)

PSWB75          	R1.5			75mm				0.85

PSWB90			R2.0			90mm				0.95

PSWBR2.5			R2.5			90mm				1.00

WALLBLOCK Batts are ideal for walls and ceilings for optimum Acoustic performance.

Special cut to size batts can a made to order to easily fit odd sizes if needed. MOQ apply